Supplementary Material

S1. Experiment

Fatigue tests were performed on hourglass-shaped specimens (Fig. S1) under uniaxial bending (β = 0°), uniaxial torsion (β = 90°), and two combinations of bending and torsion loading. Force control was applied using a single electromagnetic or inertial actuator in the fatigue stand. The driving signal was sinusoidal, defined as:

F(t) = Fa sin (2πft),

where Fa is the force amplitude, f is the loading frequency (2–30 Hz), and t is time. The actuator force was transmitted to the specimen via a lever of length L, producing a principal moment M = F·L at the specimen’s center. This moment was decomposed into bending (Mb = M cos β) and torsion (Mt = M sin β) components, where β is the angle between the specimen’s Z-axis and the lever axis. The angle β was adjustable to allow proportional combinations of bending and torsion. Fig. S1. Schematic representation of the fatigue testing configuration. The test program included constant and variable amplitude loading as follows:

• Uniaxial bending (β = 0°)

• Uniaxial torsion (β = 90°)

• Two mixed bending-torsion combinations.

Fatigue failure was defined as a reduction of 20 % in material stiffness, corresponding to a macroscopic crack length of 4–10 mm. Nominal stresses were calculated assuming isotropic, linear elastic material behavior.

S2. Material and Specimens

Specimens were machined from rolled S355 steel bars (22 mm diameter, as received). The central section was turned and manually ground with abrasive paper until the surface roughness Ra was 0.2–0.4 µm. To investigate the roughness effects, some specimens were polished with abrasive paste to a mirror finish (Ra ≈ 0.12 µm). The fatigue lives of the polished specimens fell within the scatter band of those of the unpolished specimens. The chemical composition and static strength properties of the specimens are listed in Tables S2 and S3, respectively.

Figure. S1. Geometry of the S355 steel specimen.

The fatigue dataset analysed in this work originates from multiaxial bending–torsion tests on S355 structural steel reported by Karolczuk and Kluger in the International Journal of Fatigue [Ref. X]:
A. Karolczuk, K. Kluger, Application of life-dependent material parameters to lifetime calculation under multiaxial constant- and variable-amplitude loading, Int. J. Fatigue 136 (2020) 105625. https://doi.org/10.1016/j.ijfatigue.2020.105625.
The corresponding raw experimental data have been deposited in the public Mendeley Data repository [Ref. Y] as Version 1 (published 30 March 2020), DOI: 10.17632/4tkphyg457.1 (Contributors: A. Karolczuk, K. Kluger). In the present work, these data were reformatted and filtered using the notation and screening protocol described in the Supplementary Material. Supplementary Tables S5–S7 reproduce the resulting datasets in the notation adopted in this study, together with the applied filtering criteria.

Table S2: Chemical composition of the S355 steel specimens.

| Element | C | Mn | Si | P | S | Cr | Ni | Cu | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| wt % | 0.21 | 1.46 | 0.42 | 0.019 | 0.046 | 0.09 | 0.04 | 0.17 | Rest |

Table S3: Physical properties of the S355 steel specimens

| Property | Symbol | Value | Unit |
| --- | --- | --- | --- |
| Yield strength | σy | 355 | MPa |
| Ultimate tensile strength | σu | 541 | MPa |
| Young’s modulus | E | 2.02 × 105 | MPa |
| Poisson’s ratio | ν | 0.29 | - |

Table S4: Nomenclature of applied stress components and fatigue‐life variable.

| Legend |  |
| --- | --- |
| Applied stress components |  |
| Sm - mean axial stress | bending |
| Tm - mean shear stress | torsion |
| Sa - amplitude of axial stress | bending |
| Ta - amplitude of shear stress | torsion |
| Nexp - number of cycles to failure |  |

Table S5: Original experimental dataset before filtration process: applied stress components, fatigue life, and crack outcome for all S355 specimens.

| Original row | Sm | Tm | Sa | Ta | Nexp | Crack |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.00 | 0.00 | 426.50 | 0.00 | 77730 | 1 |
| 2 | 0.00 | 0.00 | 484.34 | 0.00 | 28045 | 1 |
| 3 | 0.00 | 0.00 | 504.71 | 0.00 | 20595 | 1 |
| 4 | 0.00 | 0.00 | 557.98 | 0.00 | 8115 | 1 |
| 5 | 0.00 | 0.00 | 342.26 | 0.00 | 1252208 | 1 |
| 6 | 0.00 | 0.00 | 379.12 | 0.00 | 243816 | 1 |
| 7 | 0.00 | 0.00 | 403.05 | 0.00 | 144264 | 1 |
| 8 | 0.00 | 0.00 | 368.93 | 0.00 | 396987 | 1 |
| 9 | 0.00 | 0.00 | 390.98 | 0.00 | 198992 | 1 |
| 10 | 0.00 | 0.00 | 309.94 | 0.00 | 4274493 | 0 runout |
| 11 | 0.00 | 0.00 | 309.08 | 0.00 | 9000971 | 0 runout |
| 12 | 0.00 | 0.00 | 335.18 | 0.00 | 1528487 | 1 |
| 13 | 0.00 | 0.00 | 335.47 | 0.00 | 1444998 | 1 |
| 14 | 0.00 | 0.00 | 410.66 | 0.00 | 117275 | 1 |
| 15 | 0.00 | 0.00 | 474.06 | 0.00 | 51430 | 1 |
| 16 | 0.00 | 0.00 | 365.88 | 0.00 | 376815 | 1 |
| 17 | 0.00 | 0.00 | 390.27 | 0.00 | 192920 | 1 |
| 18 | 0.00 | 0.00 | 468.76 | 0.00 | 52000 | 1 |
| 19 | 0.00 | 0.00 | 498.45 | 0.00 | 23780 | 1 |
| 20 | 0.00 | 0.00 | 474.55 | 0.00 | 66200 | 1 |
| 21 | 0.00 | 0.00 | 483.43 | 0.00 | 19955 | 1 |
| 22 | 0.00 | 0.00 | 507.20 | 0.00 | 17012 | 1 |
| 23 | 0.00 | 0.00 | 489.63 | 0.00 | 25912.8 | 1 |
| 24 | 0.00 | 0.00 | 399.90 | 0.00 | 113900 | 1 |
| 25 | 0.00 | 0.00 | 344.92 | 0.00 | 406800 | 1 |
| 26 | 0.00 | 0.00 | 556.47 | 0.00 | 10035 | 1 |
| 27 | 0.00 | 0.00 | 0.00 | 279.00 | 8536 | 1 |
| 28 | 0.00 | 0.00 | 0.00 | 232.03 | 194605 | 1 |
| 29 | 0.00 | 0.00 | 0.00 | 245.78 | 95630 | 1 |
| 30 | 0.00 | 0.00 | 0.00 | 289.63 | 12975 | 1 |
| 31 | 0.00 | 0.00 | 0.00 | 240.83 | 140675 | 1 |
| 32 | 0.00 | 0.00 | 0.00 | 285.06 | 15500 | 1 |
| 33 | 0.00 | 0.00 | 0.00 | 185.75 | 6703466 | 0 runout |
| 34 | 0.00 | 0.00 | 0.00 | 197.29 | 6503979 | 0 runout |
| 35 | 0.00 | 0.00 | 0.00 | 224.81 | 1007493 | 1 |
| 36 | 0.00 | 0.00 | 0.00 | 222.52 | 863489 | 1 |
| 37 | 0.00 | 0.00 | 0.00 | 219.44 | 1588997 | 1 |
| 38 | 0.00 | 0.00 | 0.00 | 237.63 | 397990 | 1 |
| 39 | 0.00 | 0.00 | 0.00 | 232.85 | 311488 | 1 |
| 40 | 0.00 | 0.00 | 0.00 | 229.27 | 399999 | 1 |
| 41 | 0.00 | 0.00 | 0.00 | 244.92 | 301499 | 1 |
| 42 | 0.00 | 0.00 | 0.00 | 243.81 | 163493 | 1 |
| 43 | 0.00 | 0.00 | 0.00 | 245.50 | 217989 | 1 |
| 44 | 0.00 | 0.00 | 0.00 | 246.46 | 223989 | 1 |
| 45 | 0.00 | 0.00 | 0.00 | 256.72 | 143488 | 1 |
| 46 | 0.00 | 0.00 | 0.00 | 251.28 | 91496 | 1 |
| 47 | 0.00 | 0.00 | 0.00 | 257.75 | 109989 | 1 |
| 48 | 0.00 | 0.00 | 0.00 | 263.60 | 57890 | 1 |
| 49 | 0.00 | 0.00 | 0.00 | 264.96 | 29499 | 1 |
| 50 | 0.00 | 0.00 | 0.00 | 241.92 | 197190 | 1 |
| 51 | 0.00 | 0.00 | 0.00 | 250.47 | 211900 | 1 |
| 52 | 0.00 | 0.00 | 0.00 | 269.36 | 17760 | 1 |
| 53 | 0.00 | 0.00 | 0.00 | 230.54 | 547680 | 1 |
| 54 | 0.00 | 0.00 | 0.00 | 231.26 | 179000 | 1 |
| 55 | 0.00 | 0.00 | 303.33 | 151.67 | 364395 | 1 |
| 56 | 0.00 | 0.00 | 310.88 | 155.44 | 165191 | 1 |
| 57 | 0.00 | 0.00 | 318.55 | 159.28 | 197098 | 1 |
| 58 | 0.00 | 0.00 | 296.34 | 148.17 | 497892 | 1 |
| 59 | 0.00 | 0.00 | 321.11 | 160.55 | 169996 | 1 |
| 60 | 0.00 | 0.00 | 269.39 | 134.70 | 1842994 | 1 |
| 61 | 0.00 | 0.00 | 277.64 | 138.82 | 1001695 | 1 |
| 62 | 0.00 | 0.00 | 278.40 | 139.20 | 1040895 | 1 |
| 63 | 0.00 | 0.00 | 314.95 | 157.47 | 169494 | 1 |
| 64 | 0.00 | 0.00 | 302.76 | 151.38 | 519697 | 1 |
| 65 | 0.00 | 0.00 | 288.42 | 144.21 | 341298 | 1 |
| 66 | 0.00 | 0.00 | 281.06 | 140.53 | 439099 | 1 |
| 67 | 0.00 | 0.00 | 284.87 | 142.44 | 597091 | 1 |
| 68 | 0.00 | 0.00 | 287.42 | 143.71 | 789795 | 1 |
| 69 | 0.00 | 0.00 | 284.87 | 142.43 | 600692 | 1 |
| 70 | 0.00 | 0.00 | 282.72 | 146.38 | 697000 | 1 |
| 71 | 0.00 | 0.00 | 328.68 | 164.34 | 106099 | 1 |
| 72 | 0.00 | 0.00 | 352.25 | 176.13 | 94397 | 1 |
| 73 | 0.00 | 0.00 | 360.51 | 180.26 | 63795 | 1 |
| 74 | 0.00 | 0.00 | 401.19 | 200.60 | 14904 | 1 |
| 75 | 0.00 | 0.00 | 215.18 | 217.69 | 214493 | 1 |
| 76 | 0.00 | 0.00 | 218.58 | 221.13 | 121396 | 1 |
| 77 | 0.00 | 0.00 | 186.02 | 188.19 | 1003798 | 1 |
| 78 | 0.00 | 0.00 | 177.86 | 179.94 | 2276598 | 1 |
| 79 | 0.00 | 0.00 | 234.68 | 237.42 | 57989 | 1 |
| 80 | 0.00 | 0.00 | 235.82 | 238.57 | 60592 | 1 |
| 81 | 0.00 | 0.00 | 193.21 | 195.46 | 339795 | 1 |
| 82 | 0.00 | 0.00 | 191.53 | 193.77 | 681998 | 1 |
| 83 | 0.00 | 0.00 | 194.08 | 196.35 | 942588 | 1 |
| 84 | 0.00 | 0.00 | 196.35 | 198.65 | 516995 | 1 |
| 85 | 0.00 | 0.00 | 185.54 | 187.70 | 1287997 | 1 |
| 86 | 0.00 | 0.00 | 177.91 | 179.99 | 1111792 | 1 |
| 87 | 0.00 | 0.00 | 179.41 | 181.50 | 10000000 | 0 runout |
| 88 | 123.00 | 0.00 | 369.00 | 0.00 | 242798 | 1 |
| 89 | 124.00 | 0.00 | 372.00 | 0.00 | 311898 | 1 |
| 90 | 136.33 | 0.00 | 409.00 | 0.00 | 122893 | 1 |
| 91 | 133.00 | 0.00 | 399.00 | 0.00 | 99995 | 1 |
| 92 | 111.00 | 0.00 | 333.00 | 0.00 | 1801499 | 1 |
| 93 | 114.00 | 0.00 | 342.00 | 0.00 | 1542186 | 1 |
| 94 | 117.67 | 0.00 | 353.00 | 0.00 | 866891 | 1 |
| 95 | 118.00 | 0.00 | 354.00 | 0.00 | 626788 | 1 |
| 96 | 353.00 | 0.00 | 353.00 | 0.00 | 79693 | 1 |
| 97 | 356.00 | 0.00 | 356.00 | 0.00 | 84397 | 1 |
| 98 | 358.00 | 0.00 | 358.00 | 0.00 | 72058 | 1 |
| 99 | 335.00 | 0.00 | 335.00 | 0.00 | 128400 | 1 |
| 100 | 332.00 | 0.00 | 332.00 | 0.00 | 143087 | 1 |
| 101 | 313.00 | 0.00 | 313.00 | 0.00 | 316499 | 1 |
| 102 | 316.00 | 0.00 | 316.00 | 0.00 | 156590 | 1 |
| 103 | 300.00 | 0.00 | 300.00 | 0.00 | 1587403 | 1 |
| 104 | 316.00 | 0.00 | 316.00 | 0.00 | 717396 | 1 |
| 105 | 294.00 | 0.00 | 294.00 | 0.00 | 2235000 | 1 |
| 106 | 299.00 | 0.00 | 299.00 | 0.00 | 1601000 | 1 |
| 107 | 0.00 | 76.67 | 0.00 | 230.00 | 99000 | 1 |
| 108 | 0.00 | 68.33 | 0.00 | 205.00 | 1422090 | 1 |
| 109 | 0.00 | 69.00 | 0.00 | 207.00 | 757790 | 1 |
| 110 | 0.00 | 72.67 | 0.00 | 218.00 | 564086 | 1 |
| 111 | 0.00 | 72.67 | 0.00 | 218.00 | 320685 | 1 |
| 112 | 0.00 | 75.33 | 0.00 | 226.00 | 202991 | 1 |
| 113 | 0.00 | 67.00 | 0.00 | 201.00 | 996086 | 1 |
| 114 | 0.00 | 67.67 | 0.00 | 203.00 | 1685203 | 1 |
| 115 | 91.00 | 45.33 | 273.00 | 136.00 | 765871 | 1 |
| 116 | 94.33 | 47.00 | 283.00 | 141.00 | 523793 | 1 |
| 117 | 87.67 | 43.67 | 263.00 | 131.00 | 1270000 | 1 |
| 118 | 84.67 | 42.33 | 254.00 | 127.00 | 4656299 | 1 |
| 119 | 101.00 | 50.33 | 303.00 | 151.00 | 96505 | 1 |
| 120 | 101.00 | 50.67 | 303.00 | 152.00 | 68100 | 1 |
| 121 | 87.33 | 43.67 | 262.00 | 131.00 | 2599907 | 1 |
| 122 | 93.33 | 46.67 | 280.00 | 140.00 | 335509 | 1 |
| 123 | 97.00 | 48.67 | 291.00 | 146.00 | 302520 | 1 |
| 124 | 100.00 | 50.00 | 300.00 | 150.00 | 242823 | 1 |
| 125 | 224.00 | 112.00 | 224.00 | 112.00 | 721904 | 1 |
| 126 | 223.00 | 112.00 | 223.00 | 112.00 | 564573 | 1 |
| 127 | 238.00 | 119.00 | 238.00 | 119.00 | 371704 | 1 |
| 128 | 230.00 | 115.00 | 230.00 | 115.00 | 624804 | 1 |
| 129 | 231.00 | 115.00 | 231.00 | 115.00 | 600007 | 1 |
| 130 | 238.00 | 119.00 | 238.00 | 119.00 | 394501 | 1 |
| 131 | 223.00 | 112.00 | 223.00 | 112.00 | 1144008 | 1 |
| 132 | 222.00 | 111.00 | 222.00 | 111.00 | 2043504 | 1 |
| 133 | 58.33 | 59.67 | 178.00 | 179.00 | 818518 | 1 |
| 134 | 55.00 | 56.67 | 169.00 | 170.00 | 3841512 | 1 |
| 135 | 56.33 | 58.00 | 173.00 | 174.00 | 3105012 | 1 |
| 136 | 61.00 | 62.67 | 187.00 | 188.00 | 192004 | 1 |
| 137 | 61.67 | 63.00 | 188.00 | 189.00 | 207013 | 1 |
| 138 | 58.00 | 59.67 | 178.00 | 179.00 | 965013 | 1 |
| 139 | 166.00 | 167.00 | 166.00 | 167.00 | 194006 | 1 |
| 140 | 161.00 | 162.00 | 161.00 | 162.00 | 397702 | 1 |
| 141 | 154.00 | 155.00 | 154.00 | 155.00 | 632115 | 1 |
| 142 | 144.00 | 145.00 | 144.00 | 145.00 | 7919304 | 1 |
| 143 | 148.00 | 150.00 | 148.00 | 150.00 | 1030312 | 1 |
| 144 | 149.00 | 150.00 | 149.00 | 150.00 | 444310 | 1 |
| 145 | 160.00 | 161.00 | 160.00 | 161.00 | 382914 | 1 |

### S3. Supplementary Data S5. Dataset description and filtering protocol

- Crack classification and censoring

The raw dataset was systematically examined to ensure the integrity of the experimental fatigue data prior to modelling. Each specimen was evaluated according to its observed crack behaviour and corresponding fatigue life.

A total of five specimens were identified as runouts (crack ≠ 1), indicating that no fracture was observed within the applied number of cycles. These records were excluded from the subsequent life-regression analysis, as they represent right-censored data that could bias parameter estimation.

- Duplicate stress states

Among the specimens exhibiting valid crack events (crack = 1), several were flagged as duplicates corresponding to repeated stress-state conditions. For each group of duplicates, the first occurrence was removed to avoid over-representation of identical loading points in the dataset and to retain only independent observations.

- High-cycle outliers

In addition, three specimens were classified as high-cycle outliers with fatigue lives exceeding the predefined threshold (Nexp > 3.5 × 10⁶ cycles). These extreme observations were excluded to prevent distortion of regression parameters due to their disproportionate influence on the fitted S–N relationships.

- Summary of retained and removed specimens

Through this rule-based filtration process, the dataset was refined to retain only independent failure cases representative of the typical fatigue behaviour of S355 steel. This ensured statistical robustness and reproducibility in the subsequent modelling and analysis.

- Total original specimens: 145

- Final accepted specimens: 133

- Total removed specimens: 12

The list of removed specimens, along with the rationale for exclusion, is provided in Table S6.

Table S6. Removed specimens and reasons for exclusion

| Original row | Sm | Tm | Sa | Ta | Nexp | Crack | Reason |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 0.00 | 0.00 | 309.94 | 0.00 | 4274493 | 0 | Runout (crack ≠ 1) |
| 11 | 0.00 | 0.00 | 309.08 | 0.00 | 9000971 | 0 | Runout (crack ≠ 1) |
| 33 | 0.00 | 0.00 | 0.00 | 185.75 | 6703466 | 0 | Runout (crack ≠ 1) |
| 34 | 0.00 | 0.00 | 0.00 | 197.29 | 6503979 | 0 | Runout (crack ≠ 1) |
| 87 | 0.00 | 0.00 | 179.41 | 181.50 | 10000000 | 0 | Runout (crack ≠ 1) |
| 104 | 316.00 | 0.00 | 316.00 | 0.00 | 717 396 | 1 | First of duplicate stress state |
| 111 | 0.00 | 72.67 | 0.00 | 218.00 | 320685 | 1 | First of duplicate stress state |
| 118 | 84.67 | 42.33 | 254.00 | 127.00 | 4656299 | 1 | High-cycle outlier (Nexp > 3.5 × 10⁶) |
| 130 | 238.00 | 119.00 | 238.00 | 119.00 | 394 501 | 1 | First of duplicate stress state |
| 131 | 223.00 | 112.00 | 223.00 | 112.00 | 1144008 | 1 | First of duplicate stress state |
| 134 | 55.00 | 56.67 | 169.00 | 170.00 | 3841512 | 1 | High-cycle outlier (Nexp > 3.5 × 10⁶) |
| 142 | 144.00 | 145.00 | 144.00 | 145.00 | 7919304 | 1 | High-cycle outlier (Nexp > 3.5 × 10⁶) |

Table S7: Original experimental dataset after filtration process: applied stress components, fatigue life, and crack outcome for all S355 specimens

| Final row | Sm | Tm | Sa | Ta | Nexp | Crack | Original row |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.00 | 0.00 | 426.50 | 0.00 | 77730 | 1 | 1 |
| 2 | 0.00 | 0.00 | 484.34 | 0.00 | 28045 | 1 | 2 |
| 3 | 0.00 | 0.00 | 504.71 | 0.00 | 20595 | 1 | 3 |
| 4 | 0.00 | 0.00 | 557.98 | 0.00 | 8115 | 1 | 4 |
| 5 | 0.00 | 0.00 | 342.26 | 0.00 | 1252208 | 1 | 5 |
| 6 | 0.00 | 0.00 | 379.12 | 0.00 | 243816 | 1 | 6 |
| 7 | 0.00 | 0.00 | 403.05 | 0.00 | 144264 | 1 | 7 |
| 8 | 0.00 | 0.00 | 368.93 | 0.00 | 396987 | 1 | 8 |
| 9 | 0.00 | 0.00 | 390.98 | 0.00 | 198992 | 1 | 9 |
| 10 | 0.00 | 0.00 | 335.18 | 0.00 | 1528487 | 1 | 12 |
| 11 | 0.00 | 0.00 | 335.47 | 0.00 | 1444998 | 1 | 13 |
| 12 | 0.00 | 0.00 | 410.66 | 0.00 | 117275 | 1 | 14 |
| 13 | 0.00 | 0.00 | 474.06 | 0.00 | 51430 | 1 | 15 |
| 14 | 0.00 | 0.00 | 365.88 | 0.00 | 376815 | 1 | 16 |
| 15 | 0.00 | 0.00 | 390.27 | 0.00 | 192920 | 1 | 17 |
| 16 | 0.00 | 0.00 | 468.76 | 0.00 | 52000 | 1 | 18 |
| 17 | 0.00 | 0.00 | 498.45 | 0.00 | 23780 | 1 | 19 |
| 18 | 0.00 | 0.00 | 474.55 | 0.00 | 66200 | 1 | 20 |
| 19 | 0.00 | 0.00 | 483.43 | 0.00 | 19955 | 1 | 21 |
| 20 | 0.00 | 0.00 | 507.20 | 0.00 | 17012 | 1 | 22 |
| 21 | 0.00 | 0.00 | 489.63 | 0.00 | 25912.8 | 1 | 23 |
| 22 | 0.00 | 0.00 | 399.90 | 0.00 | 113900 | 1 | 24 |
| 23 | 0.00 | 0.00 | 344.92 | 0.00 | 406800 | 1 | 25 |
| 24 | 0.00 | 0.00 | 556.47 | 0.00 | 10035 | 1 | 26 |
| 25 | 0.00 | 0.00 | 0.00 | 279.00 | 8536 | 1 | 27 |
| 26 | 0.00 | 0.00 | 0.00 | 232.03 | 194605 | 1 | 28 |
| 27 | 0.00 | 0.00 | 0.00 | 245.78 | 95630 | 1 | 29 |
| 28 | 0.00 | 0.00 | 0.00 | 289.63 | 12975 | 1 | 30 |
| 29 | 0.00 | 0.00 | 0.00 | 240.83 | 140675 | 1 | 31 |
| 30 | 0.00 | 0.00 | 0.00 | 285.06 | 15500 | 1 | 32 |
| 31 | 0.00 | 0.00 | 0.00 | 224.81 | 1007493 | 1 | 35 |
| 32 | 0.00 | 0.00 | 0.00 | 222.52 | 863489 | 1 | 36 |
| 33 | 0.00 | 0.00 | 0.00 | 219.44 | 1588997 | 1 | 37 |
| 34 | 0.00 | 0.00 | 0.00 | 237.63 | 397990 | 1 | 38 |
| 35 | 0.00 | 0.00 | 0.00 | 232.85 | 311488 | 1 | 39 |
| 36 | 0.00 | 0.00 | 0.00 | 229.27 | 399999 | 1 | 40 |
| 37 | 0.00 | 0.00 | 0.00 | 244.92 | 301499 | 1 | 41 |
| 38 | 0.00 | 0.00 | 0.00 | 243.81 | 163493 | 1 | 42 |
| 39 | 0.00 | 0.00 | 0.00 | 245.50 | 217989 | 1 | 43 |
| 40 | 0.00 | 0.00 | 0.00 | 246.46 | 223989 | 1 | 44 |
| 41 | 0.00 | 0.00 | 0.00 | 256.72 | 143488 | 1 | 45 |
| 42 | 0.00 | 0.00 | 0.00 | 251.28 | 91496 | 1 | 46 |
| 43 | 0.00 | 0.00 | 0.00 | 257.75 | 109989 | 1 | 47 |
| 44 | 0.00 | 0.00 | 0.00 | 263.60 | 57890 | 1 | 48 |
| 45 | 0.00 | 0.00 | 0.00 | 264.96 | 29499 | 1 | 49 |
| 46 | 0.00 | 0.00 | 0.00 | 241.92 | 197190 | 1 | 50 |
| 47 | 0.00 | 0.00 | 0.00 | 250.47 | 211900 | 1 | 51 |
| 48 | 0.00 | 0.00 | 0.00 | 269.36 | 17760 | 1 | 52 |
| 49 | 0.00 | 0.00 | 0.00 | 230.54 | 547680 | 1 | 53 |
| 50 | 0.00 | 0.00 | 0.00 | 231.26 | 179000 | 1 | 54 |
| 51 | 0.00 | 0.00 | 303.33 | 151.67 | 364395 | 1 | 55 |
| 52 | 0.00 | 0.00 | 310.88 | 155.44 | 165191 | 1 | 56 |
| 53 | 0.00 | 0.00 | 318.55 | 159.28 | 197098 | 1 | 57 |
| 54 | 0.00 | 0.00 | 296.34 | 148.17 | 497892 | 1 | 58 |
| 55 | 0.00 | 0.00 | 321.11 | 160.55 | 169996 | 1 | 59 |
| 56 | 0.00 | 0.00 | 269.39 | 134.70 | 1842994 | 1 | 60 |
| 57 | 0.00 | 0.00 | 277.64 | 138.82 | 1001695 | 1 | 61 |
| 58 | 0.00 | 0.00 | 278.40 | 139.20 | 1040895 | 1 | 62 |
| 59 | 0.00 | 0.00 | 314.95 | 157.47 | 169494 | 1 | 63 |
| 60 | 0.00 | 0.00 | 302.76 | 151.38 | 519697 | 1 | 64 |
| 61 | 0.00 | 0.00 | 288.42 | 144.21 | 341298 | 1 | 65 |
| 62 | 0.00 | 0.00 | 281.06 | 140.53 | 439099 | 1 | 66 |
| 63 | 0.00 | 0.00 | 284.87 | 142.44 | 597091 | 1 | 67 |
| 64 | 0.00 | 0.00 | 287.42 | 143.71 | 789795 | 1 | 68 |
| 65 | 0.00 | 0.00 | 284.87 | 142.43 | 600692 | 1 | 69 |
| 66 | 0.00 | 0.00 | 282.72 | 146.38 | 697000 | 1 | 70 |
| 67 | 0.00 | 0.00 | 328.68 | 164.34 | 106099 | 1 | 71 |
| 68 | 0.00 | 0.00 | 352.25 | 176.13 | 94397 | 1 | 72 |
| 69 | 0.00 | 0.00 | 360.51 | 180.26 | 63795 | 1 | 73 |
| 70 | 0.00 | 0.00 | 401.19 | 200.60 | 14904 | 1 | 74 |
| 71 | 0.00 | 0.00 | 215.18 | 217.69 | 214493 | 1 | 75 |
| 72 | 0.00 | 0.00 | 218.58 | 221.13 | 121396 | 1 | 76 |
| 73 | 0.00 | 0.00 | 186.02 | 188.19 | 1003798 | 1 | 77 |
| 74 | 0.00 | 0.00 | 177.86 | 179.94 | 2276598 | 1 | 78 |
| 75 | 0.00 | 0.00 | 234.68 | 237.42 | 57989 | 1 | 79 |
| 76 | 0.00 | 0.00 | 235.82 | 238.57 | 60592 | 1 | 80 |
| 77 | 0.00 | 0.00 | 193.21 | 195.46 | 339795 | 1 | 81 |
| 78 | 0.00 | 0.00 | 191.53 | 193.77 | 681998 | 1 | 82 |
| 79 | 0.00 | 0.00 | 194.08 | 196.35 | 942588 | 1 | 83 |
| 80 | 0.00 | 0.00 | 196.35 | 198.65 | 516995 | 1 | 84 |
| 81 | 0.00 | 0.00 | 185.54 | 187.70 | 1287997 | 1 | 85 |
| 82 | 0.00 | 0.00 | 177.91 | 179.99 | 1111792 | 1 | 86 |
| 83 | 123.00 | 0.00 | 369.00 | 0.00 | 242798 | 1 | 88 |
| 84 | 124.00 | 0.00 | 372.00 | 0.00 | 311898 | 1 | 89 |
| 85 | 136.33 | 0.00 | 409.00 | 0.00 | 122893 | 1 | 90 |
| 86 | 133.00 | 0.00 | 399.00 | 0.00 | 99995 | 1 | 91 |
| 87 | 111.00 | 0.00 | 333.00 | 0.00 | 1801499 | 1 | 92 |
| 88 | 114.00 | 0.00 | 342.00 | 0.00 | 1542186 | 1 | 93 |
| 89 | 117.67 | 0.00 | 353.00 | 0.00 | 866891 | 1 | 94 |
| 90 | 118.00 | 0.00 | 354.00 | 0.00 | 626788 | 1 | 95 |
| 91 | 353.00 | 0.00 | 353.00 | 0.00 | 79693 | 1 | 96 |
| 92 | 356.00 | 0.00 | 356.00 | 0.00 | 84397 | 1 | 97 |
| 93 | 358.00 | 0.00 | 358.00 | 0.00 | 72058 | 1 | 98 |
| 94 | 335.00 | 0.00 | 335.00 | 0.00 | 128400 | 1 | 99 |
| 95 | 332.00 | 0.00 | 332.00 | 0.00 | 143087 | 1 | 100 |
| 96 | 313.00 | 0.00 | 313.00 | 0.00 | 316499 | 1 | 101 |
| 97 | 316.00 | 0.00 | 316.00 | 0.00 | 156590 | 1 | 102 |
| 98 | 300.00 | 0.00 | 300.00 | 0.00 | 1587403 | 1 | 103 |
| 99 | 294.00 | 0.00 | 294.00 | 0.00 | 2235000 | 1 | 105 |
| 100 | 299.00 | 0.00 | 299.00 | 0.00 | 1601000 | 1 | 106 |
| 101 | 0.00 | 76.67 | 0.00 | 230.00 | 99000 | 1 | 107 |
| 102 | 0.00 | 68.33 | 0.00 | 205.00 | 1422090 | 1 | 108 |
| 103 | 0.00 | 69.00 | 0.00 | 207.00 | 757790 | 1 | 109 |
| 104 | 0.00 | 72.67 | 0.00 | 218.00 | 564086 | 1 | 110 |
| 105 | 0.00 | 75.33 | 0.00 | 226.00 | 202991 | 1 | 112 |
| 106 | 0.00 | 67.00 | 0.00 | 201.00 | 996086 | 1 | 113 |
| 107 | 0.00 | 67.67 | 0.00 | 203.00 | 1685203 | 1 | 114 |
| 108 | 91.00 | 45.33 | 273.00 | 136.00 | 765871 | 1 | 115 |
| 109 | 94.33 | 47.00 | 283.00 | 141.00 | 523793 | 1 | 116 |
| 110 | 87.67 | 43.67 | 263.00 | 131.00 | 1270000 | 1 | 117 |
| 111 | 101.00 | 50.33 | 303.00 | 151.00 | 96505 | 1 | 119 |
| 112 | 101.00 | 50.67 | 303.00 | 152.00 | 68100 | 1 | 120 |
| 113 | 87.33 | 43.67 | 262.00 | 131.00 | 2599907 | 1 | 121 |
| 114 | 93.33 | 46.67 | 280.00 | 140.00 | 335509 | 1 | 122 |
| 115 | 97.00 | 48.67 | 291.00 | 146.00 | 302520 | 1 | 123 |
| 116 | 100.00 | 50.00 | 300.00 | 150.00 | 242823 | 1 | 124 |
| 117 | 224.00 | 112.00 | 224.00 | 112.00 | 721904 | 1 | 125 |
| 118 | 223.00 | 112.00 | 223.00 | 112.00 | 564573 | 1 | 126 |
| 119 | 238.00 | 119.00 | 238.00 | 119.00 | 371704 | 1 | 127 |
| 120 | 230.00 | 115.00 | 230.00 | 115.00 | 624804 | 1 | 128 |
| 121 | 231.00 | 115.00 | 231.00 | 115.00 | 600007 | 1 | 129 |
| 122 | 222.00 | 111.00 | 222.00 | 111.00 | 2043504 | 1 | 132 |
| 123 | 58.33 | 59.67 | 178.00 | 179.00 | 818518 | 1 | 133 |
| 124 | 56.33 | 58.00 | 173.00 | 174.00 | 3105012 | 1 | 135 |
| 125 | 61.00 | 62.67 | 187.00 | 188.00 | 192004 | 1 | 136 |
| 126 | 61.67 | 63.00 | 188.00 | 189.00 | 207013 | 1 | 137 |
| 127 | 58.00 | 59.67 | 178.00 | 179.00 | 965013 | 1 | 138 |
| 128 | 166.00 | 167.00 | 166.00 | 167.00 | 194006 | 1 | 139 |
| 129 | 161.00 | 162.00 | 161.00 | 162.00 | 397702 | 1 | 140 |
| 130 | 154.00 | 155.00 | 154.00 | 155.00 | 632115 | 1 | 141 |
| 131 | 148.00 | 150.00 | 148.00 | 150.00 | 1030312 | 1 | 143 |
| 132 | 149.00 | 150.00 | 149.00 | 150.00 | 444310 | 1 | 144 |
| 133 | 160.00 | 161.00 | 160.00 | 161.00 | 382914 | 1 | 145 |

Remark. The stress components (Sm, Tm, Sa, Ta) are reported here in a rounded decimal form (two decimal places) for readability and to fit within the table cells for all above tables. However, in all computational analyses, the full-precision values from the original source dataset were used.